Local dynamics of a randomly pinned crack front during creep and forced propagation:

An experimental study

Ken Tore Tallakstad1, Renaud Toussaint2, Stephane Santucci3, Jean Schmittbuhl2  and Knut Jørgen Måløy1.

1Department of Physics, University of Oslo, PB 1048 Blindern, NO-0316 Oslo, Norway

2Institut de Physique du Globe de Strasbourg, UMR 7516 CNRS, Universite ́ de Strasbourg, 5 rue Rene ́ Descartes, F-67084 Strasbourg Cedex, France

3Laboratoire de Physique, Ecole Normale Suprieure de Lyon, CNRS UMR 5672, 46 Alle d’Italie, F-69364 Lyon Cedex 07, France

ABSTRACT

We have studied the propagation of a crack front along the heterogeneous weak plane of a transparent poly(methyl methacrylate) (PMMA) block using two different loading conditions: imposed constant velocity and creep relaxation. We have focused on the intermittent local dynamics of the fracture front for a wide range of average crack front propagation velocities spanning over four decades. We computed the local velocity fluctuations along the fracture front. Two regimes are emphasized: a depinning regime of high velocity clusters defined as avalanches and a pinning regime of very low-velocity creeping lines. The scaling properties of the avalanches and pinning lines (size and spatial extent) are found to be independent of the loading conditions and of the average crack front velocity. The distribution of local fluctuations of the crack front velocity are related to the observed avalanche size distribution. Space-time correlations of the local velocities show a simple diffusion growth behavior.  We further  studied  the fluctuations of the global velocity Vl(t), computed at various length scales l, during the intermittent mode-I propagation of a crack front. The statistics converge to a non-Gaussian distribution, with an asymmetric shape and a fat tail.